## Slide 1: Effect of anisotropy on interface populations during grain growth
Debashis Kar, Seth Wilson, Gregory Rohrer, Anthony Rollett
Carnegie Mellon U
Pittsburgh, PA

## Slide 2: Preview of results
γ = 1 + *cos(4*(45-))

## Slide 3: Outline
Background
Monte Carlo model and the dual grid approach to calculate inclination
Phase field approach using interface fields
Enclosed grain shrinkage and polycrystalline growth with inclination-based anisotropy in boundary energy
Comparison of MC and PF results in 2D
Effect of anisotropic conditions at junctions on boundary evolution
Initial results in 3D

## Slide 4: Interface energy
Grain boundary energy as a function of local misorientation (Read-Shockley)
γ1 = γ0 θ (1 - ln(θ/θm)) , θ<θm
γ1 = γ0 , θ>θm
Energy as a function of grain boundary inclination
γ2 = f (ń) = 1 + cos(m),
ń is unit boundary normal vector
, degree or strength of anisotropy
, angle that GB makes with x-axis in crystal frame
Read, Shockley, Phys. Rev., 78, 275, 1950
Kazaryan, Acta mater., 50, 2491, 2002
Inclination measured from symmetric tilt boundary

## Slide 5: Simulations of anisotropic grain growth in single phase systems
(a) Initial microstructure (b) Isotropic grain growth (c) Two fold mobility anisotropy (d) Four fold energy anisotropy
Kazaryan, Acta Materialia (50), 2491-2502, 2002
Notes: Woolants paper ?

## Slide 6: Interface distributions
(a)
(b)
(c)
(a) Inclination distributions in small misorientation limit less than 5°
(b) Normalized average boundary area as function of disorientation 
(c) Energy and mobility anisotropy of similar form produce different shapes
Kazaryan, Acta materialia (50), 2491-2502, 2002
Gruber, Rollett, Acta materialia, 57(20): 6102-6112, 2009

## Slide 7: Inclination dependent interface energy
γ = f (ń) = 1 + *cos(m)
, degree of anisotropy
m, symmetry
Two energy functions
γ = 1 + *cos(4*) (top)
(minimum at 45 degs.)
γ = 1 + *cos(4*(45-))
(minimum for 90 degs.)
 = 0.1,0.2,0.3

## Slide 8: Interface energy in 3D
1 = -.5, 2 = .5
Granasy, J. Phys. Condensed Matter, 20 (2008)

## Slide 9: Monte Carlo model for anisotropic grain growth
The energy Hamiltonian considering nearest and next-nearest neighbors
Transition probability:
M E < 0
M*exp(-E/kT) E > 0
Interface energy function sum of surface energies - no binding energy, isotropic mobility (M=1)
Esurface = (γ1 + γ2) – δ (γ1 + γ2)
δ = 1 i = j
δ = 0 i ! j
Lee, Rollett, Acta materialia. 55, 615, 2007
Grest, Acta metall. 32, 783, 1984
Tikare, Acta mater. 47, 363, 1999
Von Neumann and Moore neighborhoods

## Slide 10: Interface normal calculation (dual-grid approach)
Process
Place node “A” at triple point.
Place node “B” at the centroid of this section.
Repeat for all linear segments.
The interface is defined as the piecewise linear curve that links these nodes.
A
2
1
B
Possible correction required.
KEY
Dual grid node
Dual grid cell
Interface grid node
Interface
Method developed by Steve Sintay
Notes: <number>

## Slide 11: Corrected boundary
Eliminate centroid nodes right next to triple point nodes.
Insert nodes where the reconstructed interface intersects the dual grid.
Method developed by Steve Sintay
Notes: <number>
Be aware that the the dual grid method provides an efficient and robust method of interpolating interfaces, that is bounded with respect to the image.

## Slide 12: Phase field formulation
Diffused interfaces
Energy functional defined
Allen Cahn (for non-conserved)
Cahn Hilliard (for conserved)
http://kaempfer.pirate.ch/snowpage.html

## Slide 13: Interface fields
Steinbach, Physica D 134 (1999) 385–393
Steinbach, Physica D 94 (1996) 135-147

## Slide 14: Interface fields
Steinbach, Physica D 134 (1999) 385–393
Ma, Wang, Scripta Materialia 54 (2006) 1919-1924

## Slide 15: Anisotropic shrinkage of isolated grains
γ = 1 + *cos(4*)
γ = 1 + *cos(4*(45-))
Low misorientation between grains
Notes: Energy is treated similarly to mobility (combined as a reduced mobility) in absence of junctions - hence low-energy interfaces are less mobile
Shrinking circle - volume is not conserved

## Slide 16: Anisotropic shrinkage of isolated grains (effect of misorientation)
γ = 1 + *cos(4*(45-))
Low misorientation between grains (top)
45° misorientation between grains (bottom)
A misorientation equal to half the period of the interfacial inclination energy implies interfaces at all inclinations have equal energy
Notes: Energy is treated similarly to mobility (combined as a reduced mobility) in absence of junctions - hence low-energy interfaces are less mobile
Shrinking circle - volume is not conserved. If volume is constant - Can we quantify the change in shape (away from circularity)? Is the line length of each inclination inversely proportional to the energy, as we expect?

## Slide 17: Isotropic polyxtal growth
512-squared grid, initial number of grains = 450, fiber texture

## Slide 18: How to treat junctions in the anisotropic case
Couple of approaches :
Initialise only energies between dominant fields, treat other energies unity - TJs regarded as constrained
Initialise all energies at triple junctions - extend energies along boundaries to TJs, average energy values, assume boundaries are straight till TJs - TJs regarded unconstrained
Notes: Have to discuss with seth once more about the formulation at the triple junctions

## Slide 19: Isotropic growth of sample polyxtal
Isotropic interface energy, 5 grains
256-squared grid, low misoriented boundaries
γ = 1 + *cos(4*(45-))
 = 0

## Slide 20: Anisotropic growth of sample polyxtal
Here triple junctions are isotropic
256-squared grid, initial number of grains = 5, low misoriented interfaces
γ = 1 + *cos(4*(45-))
=0.4

## Slide 21: Anisotropic growth of sample polyxtal
Here triple junctions are anisotropic
256-squared grid, initial number of grains = 5, low misoriented interfaces
γ = 1 + *cos(4*(45-))

## Slide 22: Anisotropic growth of polyxtal (effect of junctions ?)
Here triple junctions are isotropic
512-squared grid, initial number of grains = 450, fiber texture
γ = 1 + *cos(4*(45-))

## Slide 23: Anisotropic growth of polyxtal (effect of junctions ?)
Here triple junctions are anisotropic
γ = 1 + *cos(4*(45-))
512-squared grid, initial number of grains = 450, fiber texture

## Slide 24: Interface inclination distribution (MC)
Higher population of lower-energy inclinations
Fiber texture (2D), γ = 1 + *cos(4*(45-))

## Slide 25: Interface inclination distribution (phase field)
Higher population of lower-energy inclinations
Fiber texture (2D), γ = 1 + *cos(4*(45-))
Here triple junctions are treated isotropic

## Slide 26: Interface inclination distribution (phase field)
Higher population of lower-energy inclinations
Fiber texture (2D), γ = 1 + *cos(4*(45-))
Here triple junctions are treated anisotropic

## Slide 27: Effect of constraints at triple junctions on peak strength
Greater effect of anisotropy on interface population
when junctions are treated anisotropic
Kinderlehrer, Rohrer, Mat. Sci. Forum 467-470 (2004) 1063-1068
Notes: Isotropic junctions dont allow boundaries to rotate to low-energy inclinations - hence the lower peak strength - less effect of energy anisotropy on populations - need to include more slides starting with textured materials. Also have to extract stats from the (small) 3D sims .... Need some help with plotting 3D normals ....

## Slide 28: Embedded grains in 3D
Isotropic inclination energy, no misorientation between grains

## Slide 29: Embedded grains in 3D
Anisotropic inclination energy, low misorientation between grains

## Slide 30: Embedded grains in 3D
Anisotropic inclination energy, 45° disorientation between grains

## Slide 31: Inclination distribution for the embedded grain
Anisotropic inclination energy, low misorientation between grains
Similar to sims in 2D - higher energy interfaces move faster
Interfacial energy (a.u.)
Interface population (MRD)

## Slide 32: Inclination distribution for the embedded grain
Anisotropic inclination energy, 45° misorientation between grains
In crystal frame the inclination distributions are spread out
Interfacial energy (a.u.)
Interface population (MRD)

## Slide 33: Embedded grains in 3D
Anisotropic inclination energy, <45° 45° 45°> misorientation between grains

## Slide 34: Embedded grains in 3D
Anisotropic inclination energy, <45° 45° 45°> misorientation between grains

## Slide 35: Embedded grains in 3D
Anisotropic inclination energy, <45° 45° 45°> misorientation between grains

## Slide 36: Inclination distribution for the embedded grain
Anisotropic inclination energy, 45° misorientation between grains
<45° 45° 45°>, asymmetry in crystal shapes
Interfacial energy (a.u.)
Interface population (MRD)

## Slide 37: Isotropic polyxtal 3D
128-cubed, isotropic interface energy, evolved for 2000 steps

## Slide 38: Isotropic polyxtal 3D
128-cubed, isotropic interface energy, evolved for 2000 steps
(a) {100} plane (b) {010} plane

## Slide 39: Isotropic polyxtal 3D
(a) Inclination distribution at 1000 steps (b) avg. grain volume with time

## Slide 40: Conclusions
Single crystal growth under anisotropic conditions produces different interface distributions compared to what you get when they are stacked in a polycrystal
Imposing different conditions at the triple junctions produces different (stronger) boundary distributions

## Slide 41: Future work
3D polycrystalline case where junctions are treated anisotropic
Investigate why isotropic distributions are not completely flat - larger simulations or binning ?
Introduce a second phase (both grain boundaries and phase interfaces are anisotropic)

## Slide 42: Supplementary slides

## Slide 43: Grain boundary migration in isotropic MC
Site 1 has 3 unlike neighbors
Ei = 3*iso
Site 1 has 5 unlike neighbors
Ei = 5*iso
E = 2*iso (>0)
Acceptable only at higher lattice temperature (kT>0)

## Slide 44: Effect of texture on anisotropic growth
Inclination based energy anisotropy, γ = 1 + *cos(4*(45-)), anisotropic condition at junctions (a) random texture (b) sample frame
Notes: In case of random texture, since boundary energy is the sum of crystal interfaces on either side, both of these cannot in most cases achieve the lowest inclination energies at the same time, hence the lower strength in anisotropy, than say the case when all grains have identical orientation (all boundaries have low misorientation), where interfaces can rotate to inclinations which are lower in energy simultaneously in both crystal frames - hence the much stronger effect on populations

## Slide 45: Interface inclination distribution
(a) Interface energy with inclination (b) interface population with inclination (MC); population with inclination, min. energy at 0° inclinations for (c) anisotropic and (d) isotropic junctions (phase field)
Notes: Note: for certain strongly textured materials - as anisotropy strength increases so does the inverse population - more effect in case of anisotropic TJs where boundaries are freer to rotate to low-energy positions while maintaining Herrings conditions. For randomly textured materials, such a strong correlation is not observed

## Slide 46: Anisotropic polyxtal grain growth with varying conditions at TJs (sample frame)
Inclination based energy anisotropy, γ = 1 + *cos(4*(45-)), strongly textured (a) isotropic condition (b) anisotropic condition, at triple junctions
Notes: Sample texture - isotropic junctions constrain TJs to meet at 120° (or equal angles), so they cant in most cases move to the lowest energy inclinations; not the case when proper anisotropic energies are assigned to junctions so that boundaries can simultaneously rotate to certain inclinations and maintain balance of forces at the junctions

## Slide 47: Grain growth statistics
Notes: When TJs are constrained to maintain 120° and cant move to low-energy positions, irrespective of the anisotropy strength, boundaries lie along higher inclinations and move with higher velocities, giving a structure closer to isotropic growth at lower anisotropies and a comparable growth exponent

## Slide 48: Anisotropic polyxtal growth (sample frame)
Inclination based energy anisotropy, γ = 1 + *cos(4*(45-)), strongly textured (a) isotropic and (b) anisotropic energy (=0.4)
Notes: Sample texture

## Slide 49: Validation of normal calculation
Interface normals calculated for test structure
Approximate normals for grain boundary voxels close to triple junctions

## Slide 50: Grain growth statistics
Isotropic grain growth exponent higher
Anisotropic grain growth changes vertex condition, slows down grain growth
As degree of anisotropy increases, the growth rate exponent is expected to decrease(1)
(1)Grest, Acta metall. (33), 509-520, 1985
Notes: Lower reduced mobility or lower avg. GB energy (as pop. develops low energy boundaries become more populated) - so lower driving force and lower GB velocity - hence the lower exponent

## Slide 51: Steady state distribution ?
Notes: Steady state distribution after 10000 steps

## Slide 52: Interface inclination distribution (MC)
Higher population of lower-energy inclinations - both in terms of number of edges and length of those edges
Fiber texture (2D), γ = 1 + *cos(4*)

## Slide 53
dF/dp[i] += aeps*lap[j]+width*value[j]
dF/dp[j] += aeps*lap[i]+width*value[i]
Both aeps and width are scaled by energy
val = (dF/dp[i]-dF/dp[j])*M
dp/dt[i] -= val
dp/dt[j] += val
value[i,new] = value[i,old]+dt*dpdt[i]

## Slide 56: Isotropic 2D polyxtal
1024-squared grid, initial number of grains = 1500, fiber texture